## Slide 1
Ensuring fire safety in buses
Michael Försth,
Asbjørn Hagerupsen, Jan Petzäll
Informal document No. GRSG-95-30
(95th GRSG, 21 – 24 October 2008
agenda item 4)
Belgium 2003
11 dead
US Texas 2005
24 dead
Poland 2005
12 dead
Switzerland 2006
3 dead
Transmitted by the expert from Norway
Notes: Bus fire safety an issue since buses do catch fires and people die.
The problem is that the current test method does is not useful. A bus with extremely low fire safety
passes as easily as a bus with very high fire safety. Unfair.

## Slide 2: Problem: Regulation No. 118 – burning rate test
(See documents GRSG 94-33, 94-17, 93-15, 92-18, 91-19, 90-32, 90-16, 89-33, 89-23, and 88-21)
Test of horizontal flame spread (ISO 3795, FMVSS 302)
The test only considers horizontal flame propagation, and contains additional technical shortcomings such as interrupted combustion when test object burns too fast and falls apart.
Notes: This issue has been already been discussed several times here at GRSG and we will here focus on an overview of
the new proposal for Reg. No. 118.
Burning rate of 100 mm/minute is the main fire safety requirement for most buses today. All tested materials except one pass this test
Also drop test and test for curtains
Expert judgment: useless test, better not to test.

## Slide 3
Are matches fire safe?

## Slide 4: Solution: Proposed fire tests for Reg. No. 118
Use of four established ISO/CEN tests, applied world-wide:
Flame spread for surface linings
Flame spread for floorings
Test for production of smoke and toxic gases
Measurement of heat release from a seat
Evaluation of:
- Ignition and flame spread behaviour
- Smoke production
- Toxic/irritant gas generation
- Heat release from seats in real scale
These are established test methods in transportation
 Complying materials exist on the market

## Slide 5: 1. Proposed alternative test for Flame Spread
Flame spread test for surface linings
(IMO Res. A.653(16), ISO 5658-2 (2006))
Criterion: Critical Flux at Extinguishment ≥ 20 kW/m2. Same as for interior surfaces in trains and passenger ships.
Notes: Used in the IMO for passenger ships, proposed for trains in Europe.
R1 (interior surfaces) and R6 (e.g. interior of gangways).
ISO 5658-2 (2006) almost same as IMO FTP Code Resolution A.653 (16), criteria from IMO.
ISO: larger tolerances on calibration, no HRR, propane, longer flame, always flame towards object
IMO: acetylene, first two parellell flames if no ignition one flame towards object
prCEN/TS 45545-2 R1 and R6, HL2 20kW/m2, and FTP Code Res A.653(16) 10 Classification
HL2: depends on operation category and design category

## Slide 6: 2. Proposed alternative test for Flame Spread
European harmonised flooring test
(EN ISO 9239-1 (2002))
Criterion: Critical Heat Flux at extinguishment ≥ 6 kW/m2. Same as for floors and external roofs on trains.
Notes: Flooring test used for all EU and CE-marking.
ISO 9239-1 (2002)
prCEN/TS 45545-2 R7 and R9, HL2 6kW/m2

## Slide 7: 3. Proposed test for Smoke and Toxic Gas production
Smoke test and analysis of toxic gases (IMO FTP Code Annex 1 Part 2, ISO 5659-2(2006))
Criteria: Requirements on smoke density and concentration of toxic species. Same as for interior surfaces on passenger ships.
Notes: Used in IMO, proposed for trains in Europe (R1-11, R16, R19-20, R22-24). Building codes.
Underventilated  toxic gases
Criteria from IMO FTP Code Annex 1 Part 2 – Smoke and toxicity test, 2.6.1 smoke (Dm=200, bulkhead linings or ceilings) and 2.6.2 Toxicity.
CO 1450 ppm, HBr 600 ppm, HCl 600 ppm, HCN 140 ppm, HF 600 ppm, SO2 120 ppm, NOx 350 ppm

## Slide 8: 4. Proposed test for Seats
Measurement of heat release
(prCEN/TS 45545-2 Annex B)
Criterion: Maximum Average Rate of Heat Emission < 50 kW. Same as for seats on trains.
Notes: prCEN/TS 45545-2 Annex B.
Criteria MARHE < 50 kW, R17 HL2

## Slide 9: Conclusions
Buses and coaches lack requirements for an acceptable level of fire safety.
A guaranteed acceptable fire safety level, meaning similar to the level in ships and trains, can easily be achieved by ensuring that materials:
  resist fire for a longer period of time,
  produce less smoke and toxic gases.
This can be accomplished using established international fire tests, also used in other public transportation such as ship and train interiors.Therefore complying materials already exist on the market
A proposed solution is found in draft amendment to Reg. No. 118 in informal document GRSG 95-19.
This will guarantee time for evacuation, easier evacuation,
more time to extinguish the fire, decreased risk in tunnels.
Notes: Buses risk being bad guy.
Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 10: Answers to ten questions raised during 94th GRSG 21-25 April 2008
Q1:10: Do fire properties of interior materials change with age?
A: Yes. This is however traditionally not considered in fire classifications.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 11: Answers to questions raised during 94th GRSG 21-25 April 2008
Q2:10: Do fire properties of interior materials change when one material is glued onto another.
A: Yes. According to for example the CPD (Construction Products Directive) it is mandatory to test a material, or a composition of materials, in its end use configuration in order to get a correct assessment of the behaviour in fire. Alternatively the worst case can be tested, if such a case is well defined.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 12: Answers to questions raised during 94th GRSG 21-25 April 2008
Q3:10: What fire properties do glues have that is typically used in interiors?
A: Glue is not considered as a major issue from a fire safety point of view. If glue is used in compound materials it should be a part of the test object, see also question Q2. Therefore the effect of glue will be included in the test result.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 13: Answers to questions raised during 94th GRSG 21-25 April 2008
Q4:10: Do flame retardants produce toxic gases?
A: Yes in the sense that the combustion becomes more incomplete. But toxic gases are also produced in underventilated fire without flame retardants. Flame retardants are not considered as a toxic problem in fire incidents.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 14: Answers to questions raised during 94th GRSG 21-25 April 2008
Q5:10: How dangerous is smoke from fires?
A: Very dangerous. In most cases it is the fire smoke that causes death, not the flames.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 15: Answers to questions raised during 94th GRSG 21-25 April 2008
Q6:10: Can the time available for escape be increased?
A: Yes. This is very important. The proposal guarantees that the heat release rate and production of toxic gases is kept at acceptable levels, meaning similar to the case for trains and ships. Using only ISO 3795 it is not possible to recognize and avoid materials that accelerate the fire and produce toxic gases at an unacceptable rate. Almost any material is allowed according to the ISO 3795 test!
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 16: Answers to questions raised during 94th GRSG 21-25 April 2008
Q7:10: How long transition times are needed before the proposed new rules in Regulation No. 118 become mandatory?
A: This needs to be discussed with industry, authorities and other involved parties.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 17: Answers to questions raised during 94th GRSG 21-25 April 2008
Q8:10: What are the costs for developing fire safe materials that fulfil the proposed new rules in Regulation No. 118?
A: Exact cost is at the moment unknown. It depends on the willingness to adapt already existing materials for ships and trains.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 18: Answers to questions raised during 94th GRSG 21-25 April 2008
Q9:10: Can interior materials for trains and ships be approved for buses according to the proposed new rules in Regulation No. 118.
A: Yes. Since the proposed new rules and criteria are based on the requirements for ships and trains. There are many approved materials available.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.

## Slide 19: Answers to questions raised during 94th GRSG 21-25 April 2008
Q10:10: When will the standards referred to come into force.
A: The IMO FTP Code is already in force.
The standard prCEN/TS 45545-2 is soon to be finally voted.
Notes: Consequences: SP has not examined the cost consequences, but we know that this is not a large problem in other transportation sectors like trains and ships. There is also a question of cost benefit taking into account costs of fire, but this is a regulatory question.