## Slide 1: DEVELOPING FIRE TESTS FOR FCV AND HYDROGEN VEHICLES
Glenn Scheffler
Consultant for the US Department of Energy
August 2010
DEVELOPING FIRE TESTS FOR FCV AND HYDROGEN VEHICLES
SGS-10-08

## Slide 2: Compressed Hydrogen Storage System (CHSS)
Container Vessel
Container
Isolation
Valve
Fill
Check
Valve
Excess
flow
Receptacle
with check
Full System
Isolation
Low
Pressure
Regulator
PRV
PRV
High
Pressure
Regulator
Downstream Hydrogen Piping
for delivery to Fuel Cell
System or Engine
PRD
Service
Defuel
Shufoff
vent
Compressed Hydrogen Storage System
REQUIREMENT
The PRD needs to activate and vent contents during fires before the hydrogen container is weakened and bursts.
CONCERN
Localized fires can weaken the container before PRDs are activated.

## Slide 3: OVERVIEW
Transport Canada and NHTSA conducted research on localized fire test:
  Phase I: Study on current fire safety standards for containers; vehicle fire characterization, localized fire profile and test procedures.
  Phase II: Refined/simplified the test procedures and study on mitigation technology.
The research data is being used by industry to formulate localized fire test requirements and procedures.
    Defining the test article
    Establishing the test conditions
    Conducting the test

## Slide 4
  Two options are provided to the manufacturer for flexibility:
  Generic (Non-specific) Vehicle Installation
      Allows only shields and features that are attached to the vessel or system
      Size of fire set to 250mm long, covering the full diameter
      Direction and location of fire set to maximize distance from PRD(s).
  2. Vehicle-specific Installation
      Allows for thermal shields and features that are part of the vehicle
      Vehicle features may require reduction in generic fire size.
      Direction and location of fire based on the vehicle
Information on this page is still under development by industry members and organizations and should not be used until officially approved and published.
LOCALIZED FIRE TEST
Defining the Test Article

## Slide 5: Vehicle Fire Tests
      Vehicle fire tests conducted
        By JARI and US manufacturers
        Passenger vehicles, SUVs, and vans tested
      Different fires origins investigated
        Passenger compartment
        Trunk
        Wheel wells
        Pool fires beneath vehicle
        Representative localized fire test conditions were established based on data provided.
LOCALIZED FIRE TEST
Establishing Test Conditions

## Slide 6: Vehicle Fire Test Configurations
Case Number | Vehicle Type | Window Position | Fire Initiation Location | Container Location In Vehicle
1S | Sedan | Open | Cabin | In Trunk
2S | Sedan | Open | Trunk | In Trunk
3S | Sedan | Closed | Tire | In Trunk
4V | Van | Open | Cabin | Under Front Floor
5V | Van | Open | Cabin | Under Rear Floor
6V | Van | Close | Cabin | Under Front Floor
7V | Van | Close | Cabin | Under Rear Floor
8V | Van |  |  | 

## Slide 7: Vehicle Fire Tests
1) About 40% of the fires investigated resulted in localized fire conditions before conventional PRDs on end bosses would have activated.
2) While vehicle fires often lasted 30-60 minutes, the period of localized fire degradation on the storage containers lasted less than 10 minutes. See figure on next page.
3) The average maximum temperature during the localized fire period was less than 570°C with peak temperatures reaching approximately 600°C in 2 cases and 880°C in one case. See figure in two pages.
4) The rise in peak temperature near the end of the localized fire period often signaled the transition to an engulfing fire condition.
      S
Key Findings from Vehicle Fire Tests

## Slide 8: Time of Potential Localized Degradation Based on degradation starting above 300°C on container and ending when end-boss PRDs activate
Time of Localized Degradation (min)
Vehicle Fire Test Cases
(None)
(None)
(None)
(None)

## Slide 9: Average and Peak Temperatures During Localized Fire Degradation
Temperature (C)
Vehicle Fire Test Cases

## Slide 10: Vehicle Fire Tests
8-10 minutes of localized fire exposure on the test article required to cover test experience.
The selection of 600°C as the minimum exceeds the average localized temperature for all test cases.
Given that test experience indicates the controllability of the fire will be approximately ±100°C in outdoor situations, the peak temperatures expected during the proposed test will also agree favorably with test results.
      S
Rationale for Constructing the Localized Fire Temperature Profile

## Slide 11: Minimum Temperature Profile being Considered for the Localized Fire Test
3
8
800° C
Localized Fire
Engulfing Fire
Time (minutes)
10
Region of
localized impact
Regions of localized and engulfing fire impact
(1.65m max length)
600° C

## Slide 12: Vehicle Fire Tests
      LPG fuel selected for the test burner
        Fast response
        Provides controllability and repeatability
      The LPG burner for the localized fire region is lit.
        The minimum temperature profile is followed.
        Temperature in regions outside the localized fire are not specified and will vary naturally based on thermal characteristics of the container, thermal shields, and barriers.
      Test continues until the PRD activates. If necessary, the test progresses to the engulfing fire.
      Vessel burst (or significant leak) constitutes failure!
LOCALIZED FIRE TEST
Conducting the Fire Test

## Slide 13: Vehicle Fire Tests
  The “standard” engulfing fire test is still required if vehicle-specific features are utilized for the new localized fire test.
  Verification needed of the test method.
LOCALIZED FIRE TEST
Other Considerations