## Slide 1: Proposal for revising para. 2.2.1 of Regulation ECE R112 Annex 6 Zhang Heng P. R. China
Informal document GRE-68-35
(68th GRE, 16-18 October 2012,
agenda item 15)
Notes: <number>

## Slide 2: Content
What does “Resistance to atmospheric agents” mean?
Proposal to revise four(4) sections of Annex 6 para. 2.2.1.

## Slide 3: Background
Performance based
We are not going to change the current testing
We recommend describe it more accurate based on new technique development
Example of ‘temperature of boiling water’ vs. ‘100 degree C’

## Slide 4: What does “Resistance to atmospheric agents” mean?
Exposed to sunlight (especially UV radiation), temperature and moisture, automobile lenses may exhibit:
  Cracking
  Scratching
  Chipping
  Deformation
  Optical transmission decrease
  weathering

## Slide 5: Electromagnetic Spectrum
The “size”of the photon is inversely proportionate to the wavelength

## Slide 6: Shorter Wavelengths = Increased Chance of Degradation
Energy per Photon (E=hc/λ)

## Slide 7: Problem #1 -- Current Wording
The spectral energy distribution of the light source is improperly described:
2.2.1. Resistance to atmospheric agents Three new samples (lenses or samples of material) shall be exposed to radiation from a source having a spectral energy distribution similar to that of a black body at a temperature between 5,500 K and 6,000 K. Appropriate filters shall be placed between the source and the samples so as to reduce as far as possible radiations with wave lengths smaller than 295 nm and greater than 2,500 nm. The samples shall be exposed to an energetic illumination of 1,200 W/m2 + 200 W/m2 for a period such that the luminous energy that they receive is equal to 4,500 MJ/m2 + 200 MJ/m2. Within the enclosure, the temperature measured on the black panel placed on a level with the samples shall be 50 °C + 5 °C. In order to ensure a regular exposure, the samples shall revolve around the source of radiation at a speed between 1 and 5 1/min.

## Slide 8: Problem #1: Justification
Black body temperatures are useful for lighting sources and color matching, but do not accurately or sufficiently describe the sunlight spectrum
Most current international weathering standards describe the spectral energy distribution of sunlight by referring to CIE Publication No. 85:1989, Table 4

## Slide 9: Problem #1: Justification

## Slide 10: Problem #1: Proposal
Three new samples (lenses or samples of material) shall be exposed to radiation from a source having a spectral energy distribution similar to that of a black body at a temperature between 5,500 K and 6,000 K.
Change to:
Three new samples (lenses or samples of material) shall be exposed to radiation from a source having a spectral energy distribution similar to daylight spectral energy distribution described in CIE Publication No. 85:1989, Table 4.
Notes: <number>

## Slide 11: Problem #2 – Current Wording
The SPD of the light source is insufficiently defined
2.2.1. Resistance to atmospheric agents Three new samples (lenses or samples of material) shall be exposed to radiation from a source having a spectral energy distribution similar to that of a black body at a temperature between 5,500 K and 6,000 K. Appropriate filters shall be placed between the source and the samples so as to reduce as far as possible radiations with wave lengths smaller than 295 nm and greater than 2,500 nm. The samples shall be exposed to an energetic illumination of 1,200 W/m2 + 200 W/m2 for a period such that the luminous energy that they receive is equal to 4,500 MJ/m2 + 200 MJ/m2. Within the enclosure, the temperature measured on the black panel placed on a level with the samples shall be 50 °C + 5 °C. In order to ensure a regular exposure, the samples shall revolve around the source of radiation at a speed between 1 and 5 1/min.
Notes: <number>

## Slide 12: Problem #2: Justification
Providing only the wavelength range does not sufficiently define the spectrum
  It is important to accurately specify the proportions of wavelength ranges to match sunlight
  If the proportions of UV radiation do not match sunlight, unrealistic degradation may occur
This is accomplished by the use of appropriately designed “Daylight” optical filters

## Slide 13: Problem #2: Justification
Spectral passband (λ=wavelength in nm) | Minimum % | CIE No. 85:1989, Table 4 % | Maximum %
λ<290 |  |  | 0.15
290≤λ≤320 | 2.6 | 5.4 | 7.9
320<λ≤360 | 28.2 | 38.2 | 39.8
360<λ≤400 | 54.2 | 56.4 | 67.5
Table 1 – Relative spectral irradiance of xenon-arc lamps
with daylight filters (Ref. ISO 4892-2:2006)
Notes: <number>

## Slide 14: Problem #2: Justification
SAE J2527-2004 FIGURE C2 (page 17)—DAYLIGHT FILTER
VS. SUNLIGHT SPECTRAL POWER DISTRIBUTION

## Slide 15: Problem #2: Proposal
Appropriate filters shall be placed between the source and the samples so as to reduce as far as possible radiations with wave lengths smaller than 295 nm and greater than 2,500 nm, and the minimum and maximum levels of the relative spectral irradiance in the UV wavelength range are given in Table 1. (add the green font)

## Slide 16: Problem #2: Proposal
Spectral passband (λ=wavelength in nm) | Minimum % | CIE No. 85:1989, Table 4 % | Maximum %
λ<290 |  |  | 0.15
290≤λ≤320 | 2.6 | 5.4 | 7.9
320<λ≤360 | 28.2 | 38.2 | 39.8
360<λ≤400 | 54.2 | 56.4 | 67.5
Table 1 – Relative spectral irradiance of xenon-arc lamps
with daylight filters (Ref. ISO 4892-2:2006)

## Slide 17: Problem #3: Current Wording
The irradiance specification is insufficiently defined and does not conform to international standards
2.2.1. Resistance to atmospheric agents Three new samples (lenses or samples of material) shall be exposed to radiation from a source having a spectral energy distribution similar to that of a black body at a temperature between 5,500 K and 6,000 K. Appropriate filters shall be placed between the source and the samples so as to reduce as far as possible radiations with wave lengths smaller than 295 nm and greater than 2,500 nm. The samples shall be exposed to an energetic illumination of 1,200 W/m2 + 200 W/m2 for a period such that the luminous energy that they receive is equal to 4,500 MJ/m2 + 200 MJ/m2. Within the enclosure, the temperature measured on the black panel placed on a level with the samples shall be 50 °C + 5 °C. In order to ensure a regular exposure, the samples shall revolve around the source of radiation at a speed between 1 and 5 1/min.

## Slide 18: Problem #3: Justification
UV radiation is the primary cause of degradation from sunlight
Irradiance of the overall sunlight spectrum is irrelevant because it includes wavelengths that do not induce degradation
International standards solved this by specifying irradiance and luminous energy dosage at a specific wavelength in the UV region
  0.68 W/m2 irradiance at 340 nm more precisely represents the intended intensity of 1,200 W/m2 wording
  2,550 kJ/m2 at 340 nm more precisely represents the intended luminous energy of 4,500 MJ/m2 wording

## Slide 19: Problem #3: Proposal
The samples shall be exposed to an energetic illumination of 1,200 W/m2±200 W/m2, for a period such that the luminous energy that they receive is equal to 4,500 MJ/m2±200 MJ/m2.
Change to:
The samples shall be exposed to an light source with irradiance of 0.68±0.02 W/m2 at 340nm, for a period such that the radiation energy that they receive is equal to 2,550±75 kJ/m2.
Notes: <number>

## Slide 20: Problem #4: Current Wording
Exposure uniformity is not defined and hardware specific current wording violates international standards guidelines (e.g. ISO, ASTM, SAE)
2.2.1. Resistance to atmospheric agents Three new samples (lenses or samples of material) shall be exposed to radiation from a source having a spectral energy distribution similar to that of a black body at a temperature between 5,500 K and 6,000 K. Appropriate filters shall be placed between the source and the samples so as to reduce as far as possible radiations with wave lengths smaller than 295 nm and greater than 2,500 nm. The samples shall be exposed to an energetic illumination of 1,200 W/m2 + 200 W/m2 for a period such that the luminous energy that they receive is equal to 4,500 MJ/m2 + 200 MJ/m2. Within the enclosure, the temperature measured on the black panel placed on a level with the samples shall be 50 °C + 5 °C. In order to ensure a regular exposure, the samples shall revolve around the source of radiation at a speed between 1 and 5 1/min.
Notes: <number>

## Slide 21: Problem #4: Justification
The terms “revolve” and “speed” are hardware based descriptions and do nothing to ensure exposure uniformity
International standards (e.g. ISO 4892-2:2006) have solved this problem by specifying minimum uniformity

## Slide 22: Problem #4: Justification
Uniform requirements in ISO 4892-2-2006

## Slide 23: Problem #4: Justification
Uniform requirements in ISO 11341-2004
6.2 Radiation source and filter system
The irradiance E at any point over the area used for the test panels shall not vary by more than ± 10 % of the
arithmetic mean of the total irradiance for the whole area. Any ozone formed by the operation of the xenon-arc
lamps shall not enter the test chamber but shall be vented separately. If this is not possible, specimens shall
be periodically repositioned to provide equivalent exposure periods in each location.

## Slide 24: Problem #4: Justification
Figure 1 Rotating Drum Xenon Arc Tester Cross Section
Figure 2 Simple diagram of Rotating Drum Xenon
Tester chamber
a≈10 cm, b≈25 cm, c≈14 cm.

## Slide 25: Problem #4: Justification
Note: the irradiance will be higher when the sample is closer to the middle.
Figure 3 horizontal axis : Distance of point B to point A (middle)
vertical axis : Ratio of Irradiance B vs. Irradiance A (middle)

## Slide 26: Problem #4: Proposal
In order to ensure a regular exposure, the samples shall revolve around the source of radiation at a speed between 1 and 5 r/min
Change to
In order to ensure a regular exposure, the irradiance at any position in the area used for specimen exposure shall be at least 80% of the maximum irradiance.
Notes: <number>

## Slide 27: Update of para. 2.2.1 of Annex 6
2.2.1 Three new samples (lenses or samples of material) shall be exposed to radiation from a source having a spectral energy distribution similar to daylight spectral energy distribution described in CIE Publication No. 85:1989, Table 4 Appropriate filters shall be placed between the source and the samples so as to reduce as far as possible radiations with wave lengths smaller than 295 nm and greater than 2,500 nm, and the minimum and maximum levels of the relative spectral irradiance in the UV wavelength range are given in Table 1.
Notes: <number>

## Slide 28
Spectral passband (λ=wavelength in nm) | Minimum % | CIE No. 85:1989, Table 4 % | Maximum %
λ<290 |  |  | 0.15
290≤λ≤320 | 2.6 | 5.4 | 7.9
320<λ≤360 | 28.2 | 38.2 | 39.8
360<λ≤400 | 54.2 | 56.4 | 67.5
Table 1 – Relative spectral irradiance of xenon-arc lamps
with daylight filters (Ref. ISO 4892-2:2006)

## Slide 29
The samples shall be exposed to an light source with irradiance of 0.68±0.02 W/m2 at 340nm, for a period such that the radiation energy that they receive is equal to 2,550±75 kJ/m2. In order to ensure a regular exposure, the irradiance at any position in the area used for specimen exposure shall be at least 80 % of the maximum irradiance.

## Slide 30: Reference
[1] CIE Publication No. 85:1989, Table 4
[2] SAE J2527-2004 Performance based standard for accelerated exposure of automotive exterior materials using a controlled irradiance xenon-arc apparatus
[3] ISO 4892-2:2006 Plastics - Methods of exposure to laboratory light sources – Part 2: Xenon-arc lamps

## Slide 31: Questions?
Notes: <number>
Questions -- last slide before break.