PROPOSAL FOR AMENDMENTS TO i-size REGULATION

(CHILD RESTRAINT SYSTEM)

Note: The text reproduced below was prepared by the expert from CLEPA in order to better define bench foam used in this new regulation.

I.	Proposal

Annex 6 –Description of the trolley:

3.1.5.	the back and the seating shall be covered with polyurethane foam, the characteristics of which are given in Table 1. The dimensions of the cushion are given in Appendix 1 to this annex;

# Table 1

Replace”

| Density according to ISO 845 (kg/m3) [43] |  |
| --- | --- |
| Bearing strength according to ISO 2439B (N) |  |
| p – 25 per cent [125] |  |
| p – 40 per cent [155] |  |
| Bearing strength factor according to ISO 3386 (kPa) [4] |  |
| Elongation at rupture according to ISO 1798 (per cent) [180] |  |
| Breaking strength according to ISO 1798 (kPa) [100] |  |
| Compression set according to ISO 1856 (per cent) [3] |  |

«

By new table1 :”

|  | Standard | Value | Unit |
| --- | --- | --- | --- |
| density | EN ISO 845 | 68-74 | Kg/m3 |
| Compression resistance | EN ISO 3386/1 (40% compression) | 13 | kPa |
| Indentation Load Deflection (ILD) | EN ISO 2439B (40% compression) | 500 (+/15%) | N |
| Tensile strenght | EN ISO 1798 | ≥ 150 | kPa |
| Ultimate Elongation | EN ISO 1798 | ≥ 120 | % |
| Compression Set | EN ISO 1856 (22hr/50%/70°C) | ≤ 3 | % |

«

II.	Justification

The current table 1 describes former R44 foam. The informal group decided to replace R44 bench by the one defined during the NPACS project. The new table 1 defines the NPACS foam which was used by several labs during the dynamic evaluation phase of this new regulation.