## Slide 1
1. Age Influence of Wet Friction Coefficient on Test Surface
Test Tyre : 205/65R15
Informal document No. 14
(49th GRRF, 29 Jan. – 3 Feb. 2001, Agenda Item 6.2)
Reference Data for Wet μMeasurement (submitted by the experts of Japan)

## Slide 2
ABS Wet Braking Distance (V=80km/h)
ABS Wet Braking Distance (V=80km/h)
Test Tire
Car A
Car B
Car C
Car D
Test Tire
Car A
Car B
Car C
Car D
P195/75R14
ASTM
44.62
39.43
43.37
43.74
P195/75R14
ASTM
100.0
100.0
100.0
100.0
(
σ
=
0.56)
(1.00)
(0.37)
(0.95)
195/70R14
X
110.6
111.8
195/70R14
X
40.35
35.25
205/60R15
Y
112.0
129.7
117.3
122.1
(0.64)
(0.62)
205/60R15
Z
121.1
125.3
121.3
125.5
205/60R15
Y
39.82
30.40
36.98
35.82
(0.65)
(0.35)
(1.29)
(0.31)
Test Condition
Load : Ave. 390kg/tire
205/60R15
Z
36.83
31.46
35.75
34.85
IP : 180kPa (ASTM), 190kPa (A,B,C)
(0.46)
(0.41)
(0.32)
(0.45)
Water Depth : 1mm
Air Temperature : 24 - 30
℃
＊
Tire Y
≠
Tire Z in the case of Car A & B ( Level of significance : 1% )
ABS Wet Braking Distance
25
30
35
40
45
50
Car A
Car B
Car C
Car D
Braking Distance (m)
ASTM
X
Y
Z
ABS Wet Braking Distance
90
100
110
120
130
140
Car A
Car B
Car C
Car D
Braking Distance (relative %)
ASTM
X
Y
Z
2. Test Data of Stopping Distance by Using Actual Vehicles